SEMINAR

The State Key Lab of

High Performance Ceramics and Superfine Microstructure

##### Shanghai Institute of Ceramics, Chinese Academy of Sciences

中国科学院上海硅酸盐研究所高性能陶瓷和超微结构国家重点实验室

Exploration of New Crystalline Materials and Nano Materials: Structures and Properties

新型晶体材料纳米材料的探索合成结构与性能研究

Speaker

陈玲 研究员

福建物构所

###### 时间：12月8日 （星期五）上午９:30

###### 地点：2号楼607会议室

联系人：陈立东，张文清

Exploration of New Crystalline Materials and Nano Materials: Structures and Properties

Ling Chen

State Key Laboratory of Structural Chemistry, Fujian Institute of Research on the Structure of Matter, Chinese Academy of Sciences, Fuzhou, Fujian 350002,P.R. China

## Abstract

Part 1. Some binary compounds, such as Bi2Te3, CdTe, are well known functional materials; our aim is to investigate the dependence of the variation of their properties on the structure modification by introducing the transition or lanthanide metal into the binary systems. And the chemical tailoring role of the alkali metals are also introduced into the systems. Some novel series of chalcogenides, CsLnCdTe3 (Ln = La, Ln=La, Pr, Nd ,Sm ,Gd—Tm, Lu), CsGdMnTe3, Cs(M/In)9Te12 （M =Mn, Zn, Cd）were discovered. Interestingly, The exploration to the neighboring antimonide leads to the discovery of the new antimonide, Ln12Zn4Sb23 （Ln=La, Pr, Nd , Sm）and Cs8Cd16Sb30 the first transition metal involved clathrate compound. Characters in structures, properties and theoretical studies are described along the way.

Part 2. i) A new nano material synthesis methodology has been established — structure-controlled solventless method. The key point of this method is that the nanoproduct morphology is self-controlled on the atomic level by the structure of the precursor during the mild solid state conversion. Utilizing such method, we have successfully synthesized uniform Cu2S nanowires by realizing the morphology-polymerization dependence; and made monodisperse silver nanodisks from a large d-spacing layered precursor; and substantiated layered precursor- nanofilm-layered nanoproduct conversion mechanism in Bi system. ii) Utilizing solventless method we have successfully generated uniform CuS micron core-shell balls; Sb2S3, Pb5I6S2 nanobelts, (Bi(Bi2S3)9I3)0.667, Bi2S3 nanorods etc.

Part 3. The structure diversities have been found in heterometallic lead/bismuth iodides systems. A series of examples are reported for the novel [M4(bipy)12Pb11I28S]n with a 2.2 nm wide Pb/I chain, dimension-substituent relationship in [PbI(S2CNR)]n (R = Me2, (CH2)4, and (CH2)5). And a new type of compounds BiI6M3(PPh3)6 (M = Cu, Ag) exhibiting interesting ferroelectric properties is made which leads to a new access to construct/discover new ferroelectric materials. More research is ongoing.

Resume

Ling Chen, Professor of Chemistry, received her B.S. from the South-West Teacher's University (西南师大)of China in 1993, M.S. from Beijing Normal University (北京师范大学)in 1996 and Ph.D. from Fujian Institute of Research on the Structure of Matter (FIRSM,物构所), CAS, 1999. Following 3 years postdoctoral work at Iowa State University for solid state research in Ames, Iowa , USA , she joined the faculty at Fujian Institute (FIRSM, CAS) in 2003. Her group's research efforts focus on inorganic and materials chemistry dealing with synthesis, characterization and understanding of novel solid state functional materials.

陈 玲 女，1971年4月生，博士、研究员、博士生导师。1999 年中国科学院福建物质结构研究所获博士学位， 2000至2003年美国依阿华州立大学博士后，从事固态化学研究。2003年获中国科学院 “百人计划” 资助，在福建物质结构研究所工作，任课题组长，研究员。